Lecture 6

Gel Formulation

Gels

- The word ‘‘gel’’ is derived from ‘‘gelatin,’’ from the Latin word “gelu” for ‘‘frost’’ meaning ‘‘freeze’’ or ‘‘congeal

- Gels  contain both solid and liquid components.

- The solid component comprises a three-dimensional network of interconnected  molecules or aggregates that immobilizes the liquid in the continuous phase.

Gels definition

- Gels are semi-rigid systems in which the movement of the dispersing medium is restricted by the interlacing three-dimensional network of particles or solvated macromolecules of the dispersed phase.

  - Gels are usually translucent or transparent systems.

Gel and jelly

- The food industry uses the term "gelatin jelly"

- pharmaceutical industry uses the term "gelatin gel"

- Gels are generally considered to be more rigid than jellies because gels contain more covalent cross links, a higher density of physical bonds, or simply less liquid.

Advantages of gels

- Stable over long periods of time

- Good appearance

- Suitable vehicles for applying medicaments to ulcerated or burned tissues and mucous membranes because their high water content reduces irritancy.

- They give high rates of release of the medicament and rapid absorption.

- Hydrophilic gels are easily removed by gentle rinsing or natural flushing with body fluids.

Gel Uses

- Gels have a wide range of application in drug therapy and cosmetic.

- Medicated gels may be prepared for administration by various routes including topically to the skin or eye, nasally, vaginally, and rectally.

Some examples:

- Anaesthetic gels

- Acne gels

- Coal tar gels for use in treatment of psoriasis or eczema

- Spermicidal gels.

- Hair styling gels

- Sunscreen gels

- Lubricant gels

Pharmaceutical gels and their favorable  properties

Applications:                            Favorable properties

1- Dental:                                          Highly thixotropic

Optimal viscosity for filling fissures

Adherent to enamel surfaces

Optically clear

Water soluble

Orally digestible

Applications:                          Favorable properties

2- Dermatological :                        Thixotropic

Good spread ability

Greaseless (especially for acne preparations)

Easily removed

Emollient

Demulcent (especially for abraded tissue)

Non-staining

Compatible with a number of excipients

Water soluble or miscible

3- Nasal:                                          Adherent

Odorless

Non-irritating

Water soluble

4- Ophthalmic:                               Optically clear

Sterile

Mucomimetic

5- Lubricating                                Demulcent

Non-irritating or non-sensitizing

Water soluble or miscible

6- Surgical and medical procedures Lubricating

Adherent to instrument surfaces

Maximal contact with mucous membranes

Non-irritating

7- Vaginal:                                      Acid stable

Adherent

Does not liquify at body temperature

Slow dissolving

Lubricating . Greaseless and non-tacky

Non-irritating

Examples of Pharmaceutical gels

Nasal gels examples

Two nasal gels were developed and marketed.

- The intranasal vitamin B-12 gel, Nascobal (Schwarz Pharma).

- The gel base is composed of a hydrophilic cellulose derivative.

- The gel is apparently odorless and non-irritating, and adheres well to the mucous membrane.

- Neo-Synephrine Viscous (Sanofi Winthrop) is a :

- water-soluble nasal gel

- formulated with methylcellulose

- it contains the decongestant phenylephrine hydrochloride.

Gels Classification

- Organic gel

- Inorganic gel

- Organic gel: is mostly a Single-phase gels consist of organic macromolecules (proteins, polysaccharides, and synthetic macromolecules) uniformly distributed throughout a liquid in such a manner  that no apparent boundaries exist between the dispersed macromolecules and the liquid. Formation of some polymer gels is irreversible and other are reversible.

Example:

Tragacanth and carboxy methyl cellulose gels.

  - Hydrogels: are gels include ingredients that are dispersible as colloidal or soluble in water (dispersing phase is water).

  - Organogels: are gels include the hydrocarbon bases, animal and vegetable fats, soap base greases. Also

  - Hydrophilic Organogels (PEG bases) (dispersing phase is mostly oil).

- Inorganic gels (magma or milk):

- are  a two-phase gel system consists of floccules of small distinct particles (inorganic colloidal clays) rather than large molecules dispersed in a liquid and they are considered colloidal dispersions.

- The gel structure in the two-phase systems is not always stable and thus may thicken on standing, forming a thixotrope, and must be shaken before use to liquefy the gel and enable  pouring. Formation of these inorganic gels is reversible.

Example:

Milk of magnesia (or magnesia magma), which comprises a gelatinous precipitate of magnesium hydroxide in water media.

- Some terms used in gel:

- Lyophilic gelling agent: solvent loving

- Lyophobic gelling agent : solvent hating.

- Imbibition: is the taking up of certain amount of liquid without a measurable increase in volume.

- Swelling: is the taking up of a liquid by a gel with  increase in volume.

- Thixotropy: is a reversible gel-solution formation with no change in volume or temperature.

- Xerogel: is formed when the liquid is removed from a gel and only the framework  remains (e.g., gelatin sheets, acacia tears).

Gel formulation

A typical gel formulation contains:

- Water  + gelling agent

- In addition, it may contain:

- drug substance : Drugs can be suspended in the matrix or dissolved in the liquid phase.

- co-solvents (alcohol and/or propylene glycol).

- antimicrobial preservatives (methyl paraben and propyl paraben or chlorhexidine gluconate)

- stabilizers such as EDTA Na2.

Gelling agents

- The concentration of the gelling agent is mostly less than 10%,

- usually in 0.5- 2% with some exceptions.

Gelling agents commonly used are:

- Proteins (Collagen, Gelatin ).

- Natural Polysaccharides:

- Agar (from seaweed): 0.1- 1%.

- Guar gum

- Starch

- Tragacanth gum: gel stable at pH 4 -8, preserved by 0.1% benzoic acid or Na benzoate or combination, or PP +MP 0.2%, pre wetting powder with PG, Ethanol, glycerin.

- Pectin

- Alginic acid (from seaweed): 1-5%, swells in water 200-300 times of its weight, viscosity increased by adding calcium salts.

- Cellulose derivatives:

- carboxy methyl cellulose: 4- 6%, glecerin may be added to prevent drying, stable in pH (2- 10), incomputable with ethanol.

- carboxy methyl cellulose sodium: can be dispersed in cold water with high shear, stable in pH (5- 10).

- Methyl cellulose: 5%, hydrate slowly, compatible with anhydrous alcohol, PG may be used to wet the powder. Electrolyte increase viscosity.

- Synthetic macromolecules:

- Carbomer (carbopol):

high molecular- weight water-soluble polymers of acrylic acid cross-linked with allyl ethers of sucrose and/or pentaerythritol), white dry powder,

its aqueous dispersion pH 2.7- 3.5, used concentration 0.5–2.0% in water, added very slowly into water and very rapidly stirring.

Neutralized using NaOH, TEA (up to 50% alcohol)

Gel viscosity is affected by pH (4.5- 5, max viscosity at 7), elecrolytes (max. 3% may be added).

Carbomer types:

- 910 (low viscosity formulations, suspension preparation, effective at low concen.).

- 934 (thick formulation, viscous gel preparation, sustained release products)

- 934P (similar to 934, but for oral and mucosal preparations)

- 940  yields the highest viscosity,  between 40,000 and 60,000 CP as a 0.5% aqueous dispersion., can be prepared using  hydroalcoholic solutions (reduce viscosity)

- Poloxamer (POE + POP copolymer) 124, 237, 407 (Pluronic, USA):

15- 50%, gels are stable in presence of acids, alkalis and metal ions,

- Polyvinyl alcohol (PVA):

2.5%, dry rapidly when apply to the skin, borax is a good agent for gelling PVA, disperse in cold water followed by hot water

- colloidal silicon dioxide:

- absorb large quantity of water, viscosity affected by temp., pH 7.5, gel in more hydrophobic.

- -Aluminum stearate (Alugel):1 -2% for mineral oil

- Microcrystalline waxes

- inorganic colloidal clays:

Magnesium aluminum silicate (Veegum), 10%, best pH >3.5, bind with some drugs.

- Aluminum hydroxide

- Bentonite (aluminum silicate)

- Laponite (Magnesium silicate)

- magnesium hydroxide

- Surfactants (e.g.  Brij).

- others: cetostearyl alcohol

- Gel-forming hydrophilic polymers are typically used to prepare lipid-free semisolid dosage forms, including dental, dermatological, nasal, ophthalmic, rectal, and vaginal gels.

- Gel-forming Surfactants are typically used in hair styling gels.

Gelling concentrations for substances used in pharmaceutical products

Substance Gel-forming                                     concentrations (wt %)

Proteins

Collagen                                                                                       0.2–0.4

Gelatin                                                                                              2–15

Polysaccharides

Agar                                                                                                 0.1–1

Alginates                                                                                          0.5–1

K-Carrageenan                                                                                   1–2

Guar gum                                                                                       2.5–10

Hyaluronic acid                                                                                   2

Pectins (low methyoxy)                                                                   0.8–2

Starch                                                                                                   6

Tragacanth gum                                                                                  2–5

Semisynthetic polymers (cellulose derivatives)

Carboxymethylcellulose                                                                     4–6

Hydroxypropylcellulose                                                                   8–10

Hydroxypropylmethylcellulose                                                        2–10

Methylcellulose                                                                                  2–4

Synthetic polymers

Carbomer                                                                                          0.5–2

Poloxamer                                                                                        15–50

Polyacrylamide                                                                                    4

Polyvinyl alcohol                                                                             10–20

Inorganic substances

Aluminum hydroxide                                                                          3–5

Bentonite                                                                                                5

Laponite                                                                                                  2

Surfactants

Brij

Example 1:

Carbomer 941 gel

Carbomer 941                                           0.5 (% w/w)

Glycerine:                                              10.0  (% w/w)

Triethanolamine                                       0.5 (% w/w)

Water                                                      89.0 (% w/w)

Preservative                                            q.s.

- Preparation procedure:

- Water, glycerine, and preservative are mixed

- and the carbomer added by sprinkling on the surface while constantly mixing at high speed.

- Triethanolamine is added with slow agitation until a clear viscous gel forms.

Example 2:

Carbomer 934 alcoholic gel

Carbomer 934                             3.0 (% w/w)

Glycerine                                   10.0 (% w/w)

Ethanol                                      40.0 (% w/w)

2-Ethyl hexylamine                     2.5 (% w/w)

Water                                          44.5 (% w/w)

- Preparation procedure:

- Glycerine and water are mixed.

- The carbomer is dispersed in the glycerine and water mixture by sprinkling on the surface while constantly mixing at high speed.

- 2-ethylhexylamine and ethanol are mixed.

- and a solution of the 2-ethylhexylamine in ethanol is added to the water solution with mixing until a clear transparent gel is formed.

Emulgel and Emulgin

- EMULGELS are emulsions, either of the oil-in-water or water-in-oil type, which are gelled by mixing with a gelling agent.

- They have a high patient acceptability since they possess advantages of both emulsions and gels (e.g. Voltaren emulgel).

EUMULGIN are an ethers consist of (fatty alcohol + PEG polymer)  used as nonionic surfactant

Examples:

EUMULGIN® L (PPG-1-PEG-9 Lauryl Glycol Ether) is a clear, slightly turbid, light yellow liquid product, with a distinctive odour. The product is used as a non-ionic O/W emulsifier and/or solubiliser.

EUMULGIN® S2 (Polyoxyethylene Stearyl Ether) is a white solid ,with a faint characteristic odour, it is used as a non-ionic emulsifier for cosmetic and pharmaceutical creams and lotions.

Done by : Ahmad Mahrouseh . Emad Swwas